## Slide 1: Lecture 4: Collective Phenomena

## Slide 2: Collective phenomena
cross section
A notched bcc Fe single-crystal is subjected to a high rate of tensile deformation.

## Slide 3: Collective phenomena
cross section
A notched bcc Fe single-crystal is subjected to a high rate of tensile deformation.

## Slide 4: Collective phenomena
stress (GPa)
elongation
1.2 x
1.4 x
1.6 x
0.5
1.0
1.5
2.0
A notched bcc Fe single-crystal is subjected to a high rate of tensile deformation.

## Slide 5: Collective phenomena
stress (GPa)
1.5 x
2.0 x
2.5 x
0.5
1.0
1.5
2.0
2.5
3.0 x
elongation
A notched bcc Fe single-crystal containing bcc W inclusions is subjected to a high rate of tensile deformation.
W inclusions

## Slide 6: Collective phenomena
The defect-free crystal failed without
necking at the points of fracture
no change in cross-section
The crystal with W-inclusions failed after significant necking
change in cross-section
brittle fracture
ductile fracture
The mechanical properties of a component are dependent on its microstructure.
For example, depending on its content of dislocations, precipitates, point defects, grains, etc., the same material can behave brittle or ductile.
stress (GPa)
1.5 x
2.0 x
2.5 x
0.5
1.0
1.5
2.0
2.5
3.0 x
elongation
brittle
ductile
J. Glassman et al. (2020). Constr. Steel Res. 165

## Slide 7
Studying some of the more interesting collective phenomena require propagating millions of atoms over millions of time-steps.
As the time to evaluate DFT forces scales with , we hit a wall: Instead, we describe interatomic forces by a classical potential.
For example, in the Embedded Atom Method (EAM), the energy of the atom is given by:
pairwise
short-ranged
many-body
short-ranged
Molecular dynamics
atom j
nebs(j)
Rcutoff
Rjk
atom k
out of range atoms
Right: Interatomic forces are short-ranged; a given atom j is only affected by the forces of atoms k within a range of Rcutoff.
Assuming atoms move slowly and electrons do not get excited (i.e. we remain in the ground-state adiabatically), we can propagate atomic trajectories following Newton’s equation of motion:
Right: An initially dis-ordered configuration of tungsten is quenched over 10 picoseconds.
Atoms are coloured by their potential energy.
M. W. Finnis and J. E. Sinclair (1984), Phil. Mag A 50.1: 45-55
a typical time-step is of order 1 fs = 10-15s

## Slide 8
CPU 1
CPU 2
CPU 3
CPU 4
CPU 5
CPU 6
CPU 7
CPU 8
CPU 9
CPU 10
CPU 11
CPU 12
CPU 13
CPU 14
CPU 15
CPU 16
Right: MD parallelisation illustrated for 16 CPUs: the simulation cell is split into a domains, one per CPU. Each CPU only evaluates forces in its own domain.
Studying some of the more interesting collective phenomena require propagating millions of atoms over millions of time-steps.
As the time to evaluate DFT forces scales with , we hit a wall. Instead, we describe interatomic forces by a classical potential.
For example, in the Embedded Atom Method (EAM), the energy of the atom is given by:
pairwise
short-ranged
many-body
short-ranged
Assuming atoms move slowly and electrons do not get excited (i.e. we remain in the ground-state adiabatically), we can propagate atomic trajectories following Newton’s equation of motion:
M. W. Finnis and J. E. Sinclair (1984), Phil. Mag A 50.1: 45-55
atom j
nebs(j)
Rcutoff
Rjk
atom k
out of range atoms
Right: Interatomic forces are short-ranged; a given atom j is only affected by the forces of atoms k within a range of Rcutoff.
Molecular dynamics
a typical time-step is of order 1 fs = 10-15s

## Slide 9
CPU 1
CPU 2
CPU 3
CPU 4
CPU 5
CPU 6
CPU 7
CPU 8
CPU 9
CPU 10
CPU 11
CPU 12
CPU 13
CPU 14
CPU 15
CPU 16
Right: MD parallelisation illustrated for 16 CPUs: the simulation cell is split into a domains, one per CPU. Each CPU only evaluates forces in its own domain.
LAMMPS Molecular Dynamics Simulator
Analysis and visualisation: OVITO
Free, open source, highly scalable on CPUs & GPUs
atom j
nebs(j)
Rcutoff
Rjk
atom k
out of range atoms
Right: Interatomic forces are short-ranged; a given atom j is only affected by the forces of atoms k within a range of Rcutoff.
Molecular dynamics

## Slide 10
Two examples of MD applied to fusion materials
2H
3H
n (14.1 MeV)
4He (3.5 MeV)
Deuterium-Tritium fusion
(100 million Celsius)
neutron
flux

## Slide 11
100 keV Collision Cascade in tungsten
32 nm
0.316 nm
BCC unit cell
(2 mio atoms)

## Slide 12
100 keV Collision Cascade in tungsten
100 keV
32 nm
(2 mio atoms)
0.316 nm
BCC unit cell

## Slide 13
100
10
0
-100
-10
Pressure (GPa)
100 keV Collision Cascade in tungsten
0.0002 dpa

## Slide 14
100 keV Collision Cascade in tungsten
crowdion
vacancy
<111> cluster
1.6
0
excess potential energy (eV)
0.8
0.0002 dpa

## Slide 15
Computer time required to reach 1 dpa:
  50,000 CPU-hours
  i.e. ~1% of a typical HPC allocation
High-dose simulations require access to high performance computing facilities.
Simulated dose-rate:
Experimental dose-rate:
14 orders of magnitude difference between simulated and exp. time!
interstitials
vacancies
<111> dislocations
<100> dislocations
Mason et al. (2020) PRL 125.22: 225503

## Slide 16
https://developer.nvidia.com/hpc-application-performance
toy potential
empirical potential
machine-learned

## Slide 17
On the range of validity of high-dose simulations
Microstructure evolves on multiple starkly different timescales.
See simulated post-irradiation annealing of a W single-crystal (dose 0.32dpa, ramping rate 2.5 x 1011 K/s)
Most recovery occurs at about 0.75eV, consistent with stage-III recovery
There is a large spectral gap from 0.10eV to 0.45eV; in between interstitials and vacancies becoming mobile, not much else happens
In conclusion, cascade simulations generate microstructures consistent with the earlier recovery stages
spectral gap
spectral gap
Boleininger et al. (2023) Sci. Rep. 13 (1): 1684

## Slide 18
  Irradiation is well known to enhance creep rates; conventional models creep rates increase with temperature.
Gilbert (1977), Measurement of Irradiation-enhanced Creep in Nuclear Materials, 204-209
316 SS
Effective creep strain (%)
Temperature (℃)
1000/T (K-1)
in-vessel creep
fluence
thermal
creep
time
Low temperature irradiation creep
What happens at lower temperature?
Creep in a He-pressurised tube in a test reactor is
measured by the change in circumference
press. gas
metal tube

## Slide 19
  Irradiation creep at 8 dpa in pressurised steel tubes, 60-125 appm He
Griffiths (2019) Structural Alloys for Nuclear Energy Applications
60 ℃
300 ℃
  Stress relaxation for Inconel-750X bent beams in NRU
60 ℃
330 ℃
400 ℃

## Slide 20
Rotary stage
Load cell
Sample
Rotary stage
Linear actuator
20.5 MeV
W6+ ions
mechanical load
General-purpose irradiated fiber and foil experiment
Johann Riesch, Alexander Feichtmayer, and others, at IPP Garching
Cost-effective and surrogate for reactor conditions using high-energy ions from a particle accelerator under simultaneous loading by:
  mechanical loading and tensile testing
  cooling or heating
  low energy deuterium or helium plasma
  Alexander Feichtmayer,
  PhD Candidate
  Dr. Johann Riesch
thin tungsten wire
The GIRRAFE experiment

## Slide 21
In-situ irradiation creep experiment
0 MPa
16 µm
15 mm
Credit: Robert Lürbke | IPP

## Slide 22
0 MPa
1000 MPa
16 µm
15 mm
Credit: Robert Lürbke | IPP
In-situ irradiation creep experiment

## Slide 23
20.3 MeV W6+
0 MPa
1000 MPa
970 MPa
heating
16 µm
15 mm
Credit: Robert Lürbke | IPP
In-situ irradiation creep experiment

## Slide 24
20.3 MeV W6+
0 MPa
1000 MPa
970 MPa
990 MPa
heating
16 µm
15 mm
Credit: Robert Lürbke | IPP
In-situ irradiation creep experiment

## Slide 25
20.3 MeV W6+
0 MPa
1000 MPa
970 MPa
990 MPa
heating
repeat
16 µm
15 mm
Credit: Robert Lürbke | IPP
In-situ irradiation creep experiment

## Slide 26
20.3 MeV W6+
0 MPa
1000 MPa
970 MPa
990 MPa
heating
6 dpa
repeat
16 µm
15 mm
Credit: Robert Lürbke | IPP
In-situ irradiation creep experiment

## Slide 27
  Left: Simulation of single-crystal W subjected to recoil energies consistent with 20.3 MeV W6+ self-ion irradiation. A fixed uniaxial stress is maintained, and zero stress elsewhere.
  Right: Eigenstrain surrogate model from maximum likelihood estimation, described by , where and are functions of dose and external stress .
Surrogate model driven by molecular dynamics
  We use MD as a “black box” model to generate the materials data:
  For a given constant external stress , the surrogate model returns eigenstrain as a function of irradiation dose .
Boleininger et al. (2022) PRMat. 6 (6): 063601
Feichtmayer et al. (2024) Comm. Mater. 5.1: 218

## Slide 28
1. The eigenstrain is expressed as a body-force:
propagate time
  The eigenstrain model is embedded into an isotropic linear elastic medium, as a property of each FEM node.
  The dose-rate profile drives the accumulation of eigenstrain across the wire cross-section.
“Digital shadow:” multiscale irradiation creep model
20.3 MeV
W6+ ions
1.2
0
y
x
(dpa/h)
Simulated exposure profile (SRIM)
0 µm
8 µm
The surrogate model does not account for the general stress history. We assume that eigenstrain accumulates irreversibly w.r.t. stress.
Da Fonseca et al. (2023) Scripta Mater. 233: 115510
2. And embedded into linear elasticity:
3. Here, eigenstrain is assumed to accumulate irreversibly:
Reali et al. (2021) Nucl. Fus. 61.1: 016002
Feichtmayer et al. (2024) Comm. Mater. 5.1: 218

## Slide 29
Example: Multiscale irradiation creep model
  Bringing it all together, the virtual experiment can predict the experimental outcome － without adjustable parameters
  In the irradiated layer, the elastic stress is entirely compensated by the irradiation-induced eigenstrain.
  Within half an hour, most of the stress has relaxed (=0.5 dpa in the Bragg peak)
  Simulated relaxation is overestimated by 20% compared to experiment

## Slide 30: Example: life-time analysis of an allotrope in iron
C15 structures are the most stable interstitial-type defect in bcc-Fe, so we would expect it to form under irradiation.
However, we also know that it collapses into other defects at higher temperature. Can we estimate its mean life-time?
Marinica et al, PRL 108, 025501 (2012)
Alexander et al, PRB 94, 024103 (2016)
C15
½<111>
Swinburne and Marinica, PRL 120, 135503 (2018)

## Slide 31: Example: life-time analysis of an allotrope in iron
First, we run cascade simulations with recoil energies consistent with 10 MeV Fe ion-irradiation at
We see C15 clusters forming, with the population reaching a dynamic steady state at high dose
While C15s of size should be nominally stable at irradiation triggers their untimely collapse
We note that 10 MeV ion-irradiation is leads to quite large cascades. Perhaps larger clusters could form under electron-irradiation?
0.1 dpa
atom in a C15 environment
self-interstitial atom
-dislocation

## Slide 32: Example: life-time analysis of an allotrope in iron
We shall focus on C15 clusters of size 50 and size 100.
We ran MD simulations to study the collapse of and clusters at various temperatures under zero pressure.
To get a picture of the collapse statistics, each temperature was sampled 10 times with a simulated time of 10 ns.

## Slide 33: Example: life-time analysis of an allotrope in iron
The collapse occurs through multiple stochastic transitions between metastable configurations. The collapse does not always conclude within 10 ns.
An estimation of the transformation time requires a statistical treatment accounting for the chances of collapse and survival of the cluster
The life-time of the cluster is modelled by an Erlang distribution (accounting for multiple transf. steps):
where
is the expected step transformation rate
is the number of transformation steps

## Slide 34: Example: life-time analysis of an allotrope in iron
For given temperature, the probability of an observed simulation outcome of cluster collapses and survivals with times and is:
For a cluster of a given size, across all simulations of varying temperatures, the joint probability of the simulation outcome is:
By maximising the log-likelihood , we obtain and . We can also extrapolate cluster life-times towards lower temperatures, including uncertainties (Metropolis-Hastings)
C15 clusters appear to be quite stable at room temperature… unless they grow too big!